Competitive Growth between Two Converging Dendrites

using Mat IC software

Introduction:

A wide range of axial orientations can be produced during the directional solidification of highly alloyed Ni-base superalloys depending on the efficiency of the competitive growth mechanism. In a second generation Ni-base superalloy such as CMSX-4, misaligned grains may deviate by up to 15º from the <001> orientation as illustrated in Figure 1. Overgrowth of the lagging dendrite can occur by a combination of physical blocking or by enrichment / depletion of the solute, depending on the nature of partitioning, which subsequently retards its growth. The aim of this tutorial is thereby to simulate the competitive growth between two converging dendrites. It is expected that one of these dendrites will eventually overgrow the other.

Usage in this tutorial

Commands that you type are printed in:

courier 10 pt

Computer commands enclosed in anglebrackets <> should be replaced with your own choice for file name, directory name etc. Do not type the anglebrackets. File and directory names should not have contain spaces or other special characters.

Figure 1: Optical micrograph of two converging dendrites.

# Getting started…

## Suggested Software

Your computer should be running a 'posix' type of environment, either a Gnu/Linux system, a UNIX type system, or the Gnu/Cygwin package on Microsoft Windows platforms.

You will need some software for viewing image and two- and three-dimensional binary files, we use the Quick Image Viewer and ImageJ, these are available from:

qiv: http://www.klografx.net/qiv/

ImageJ: http://rsbweb.nih.gov/ij/

These or similar programs  may also be available as part of the Gnu/Linux distribution or may be bundled with your system.

- Preparation of the working directory: The first step in the simulation is to create a sub-directory in a scratch directory;  something like /jobs/<user-name>/test_bicrystal or /workdir/<user-name>/test_bicrystal,  where the simulation will be run.  Your system administrator may have some requirement for the location of working directories. If you are using your own system, be aware that some choices of input may result in large quantities of output and may fill up the disk; if multiple disks or partitions are available you should use a 'non-system' disk or partition.

- Copy the executable and input files to the test directory: Files are located in the folder

tutorials/BicrystalTutorialFiles/

in the documentation package.

- Checking the input files: the following three input files are necessary to run a job (Table I): umat_ctrl.in, umat_geoplus.in, and umat_matprop.in.

Table I. Input files and their descriptions

| umat_ctrl.in | The main control files including alternate filenames other files |
| --- | --- |
| umat_geoplus.in | The geometry and boundary/initial conditions |
| umat_matprop.in | Global properties of the materials and nucleation model inputs |
| props_alloy0.in | Properties that apply only to the first alloying solute |
| props_alloy1.in | Properties that apply only to the second alloying solute (not used in this example) |
| props_gas.in | Properties that apply only to the gas solute |

- umat_ctrl.in. All the control options are given in this file. The coordinates of the fixed nucleation sites for the two seed dendrites are specified by the FixedNuc option. A fixed nucleation site can be activated by simply removing the pound sign (#) in front of the FixedNuc identifier. In total, there are 8 numbers to be entered for each fixed nucleation site. The first three numbers correspond to the x, y, and z coordinates. The next three numbers correspond to the angle the growth direction of the new grain makes with the <001> orientation. A critical undercooling value can be entered in place of the seventh number. The last number corresponds to the nature of the cell, or the phase associated with the solid in it. A value of 0 is associated with the primary phase. The umat_ctrl.in file used in this simulation will activate two fixed nucleation sites, which are located at (20,0,0) and (60,0,0). And the two crystals grow with misorientations of 10 and 140, as indicated below. User should make sure that the nucleation site for the dendrite will lie inside the domain, as it is mentioned in the following paragraph.

- umat_geoplus.in. All of the geometry and output data are given in this file. The size of the domain in the x, y and z directions is specified by the three numbers after the keyword NCellsPerSB. The user must make sure that the domain size is sufficient to allow the 2 dendrites to grow within the set domain. The amount of time allowed to finish the job is given by the keyword FinishTime. The size of CA cells is defined by CellSize and TimeStep is the calculation time step in seconds, both of which are also important variables that may be changed prior to a simulation.

- umat_matprop.in. All of the material property data related to the nucleation module can be found in this file. The density of the nucleation sites can be adjusted by changing the keyword MaxGrainDensity. The value of the mean critical undercooling, GNGaussCentre, and the standard deviation, GNGaussSigma, associated with the Gaussian distribution function can also be modified. Both of these parameters determine the distribution of critical undercoolings allocated to the potential nucleation sites within the molten alloy.

Running the code:

- Launching a simulation: The code be run by any of the following commands:

umat_run  -c   <name of the control input file>

e.g. 	umat_run -c umat_ctrl.in

Viewing the results:

- Viewing the microstructural evolution with qiv: Once the simulation has finished, the evolution of the dendritic front with time can be observed by viewing the generated .png files.

The unzipped .png files can be viewed with the qiv (quick image viewer) command:

qiv -w200 cr_4s*.png

The –w200 option specifies the width of the viewing window. The size of the window used to visualize the results can be adjusted by changing the number in the command line. cr_4s*.png indicates all of the .png files that begin with cr_4s. Once the viewing window is open, pressing the spacebar will load the image corresponding to the next time step.

The files have the form: <basename>_<blocknum>t<timestep>.png, the example of the file name is: cr_4s_sb0s0t00008300.png.

Hence, the evolution of the solidification microstructure may be observed over time, as illustrated in Figure 2.

| (a) Time = 1.2s | (b) Time = 4.9s | (c) Time = 6.9s |
| --- | --- | --- |
| Figure 2: Predicted results of competitive growth for two converging grains with misorientations of 10 and 140, respectively. |  |  |

- Opening binary files with ImageJ: Binary files (*.bin) that are generated during the CAFD simulation may be opened in ImageJ, which can be downloaded for free online, at: http://rsb.info.nih.gov/ij/.

Each binary output files contain the raw data for one variable in a selected 2-dimensional (x-y) slice of the micromodel domain. The file name is of the form

<FirstPrefix>_<SecondPrefix>_<basefilename>_<timepoint>.bin

The data type of the data is indicated by FirstPrefix, and the variable is indicated by SecondPrefix in the file name, as given in Table II.

Table II. Input files and their descriptions

| FirstPrefix |  |
| --- | --- |
| F | floating point type (single or double depends on compilation) |
| I | integer type, e.g. grain number |
| SecondPrefix |  |
| A | Alloy solute |
| G | Gas solute |
| FS | Fraction Solid |
| UC | undercooling |

These *.bin files can be visualized after importing them to ImageJ  by clicking on File->Import->Raw (see Figure 3).

Figure 3: Import binary file into ImageJ.

As an example, the binary file corresponding to the equivalent concentration or the fraction of solid after 3.7 seconds (F_EQ_cr_4s_sb0s0t000003700.bin or F_FS_cr_4s_sb0s0t000003700.bin) can be viewed by ImageJ, the dialogue showed in Figure 4 will pop out, and the type and dimensions must then be inputted. The width and height should match the size of the domain set in the ca_geoplus.in input file.

Figure 4: Importing a binary file in ImageJ

After entering the correct information, click on OK. The image shown in Figure 5 should be displayed.  The detailed methods of analyzing the binary files are available at:  http://rsb.info.nih.gov/ij/docs/menus/analyze.html

| (a) Equivalent concentration at 3.7s | (b) fraction of solid at 3.7s |
| --- | --- |
| Figure 5: Bi-crystal region using ImageJ. |  |